Process Spec:		Procedure for Rod Insertion

Components:		Matrix assembly

Tungsten rods wound with thermo-formed PEEK fibres

Material:			Latex Gloves

Ethanol

Swabs

Tooling:			Rod Insertion Tool (Bullet)

Fiber cutters

HV Test Apparatus

Compressed N2 Nozzle

Red Parts Bin

QC Data Sheet:		Rod Insertion & HV Logsheet

Process:

- Position one person at each module face. Wear gloves throughout this process.

- Swab the tube with ethanol. Give a 2 second blast from N2 nozzle down tube interior to remove any dust.

- Select rod from the rack and slip the rod insertion bullet over signal pin onto the rod.

- Hold the rod perpendicular to the endplate over the tube and carefully insert the bullet into the tube. Do not rotate the rod during insertion.

- Remove the bullet as it emerges from the tube. Examine the bullet for copper particulate. Wipe the bullet clean with ethanol.

- Cut off fiber so as to leave ~3 cm of fiber protruding from tube.

- Repeat until rod insertion of the row of tubes is complete.

- Record all work in the Assembly Logbook