Process Spec:	 	QC Inspection for Tube Deburring

Components:		Copper Tubes, deburred

Materials:			latex/nitrile gloves

Tools:			Shop Microscope

Lamp

QC Data Sheet:		Tube Processing Tag

Process:

- Wear gloves during this procedure.

- Obtain a bin of deburred copper tubes.

- Select 12 tubes at random from the bin and examine both ends under the microscope at 100x.

- Examine for flaws such as metal flakes, curls or balls along the inner and outer radii of the tube.

- Reject any tubes that are not properly deburred. The rejected tubes should be reprocessed. If more than 3 of the 12 selected tubes are rejected, then return the whole batch for reprocessing.

- Fill in the Tube Processing Tag.