##### Process Spec:		Procedure for Tube Cleaning

Components:		Copper Tubes

Materials:			Latex Gloves, Heavy Chemical Gloves

### Citranox Cleaner, LPS Cleaner

Reverse Osmosis Water, Foam swabs

Tooling:			Ultrasonic Cleaners

Cleaning Racks, Rinsing Tanks, Bag heat sealer

QC Data Sheet:		Quality Control of Tube Cleaning

###### Materials Cleaning Report

Tube Processing Tag

Process:

Wear gloves whenever tubes are being handled.  Heavy chemical gloves can be worn when handling hot objects, or when handling mineral spirits.

- - Preparation Stage -

  - Pre-soak the tubes in mineral spirits for a minimum 7 days.

  - Swab out the tubes, 2 swabs each tube.

  - Load 124 tubes into the washing rack, and stand to dry.

  - Place the rack of tubes into 1st ultrasonic cleaner. Agitate with ultrasound for 60 minutes in LPS (20% soln., 65o C).

  - Soak the tubes in LPS solution for 12 hours (overnight).

- - 1st Cycle –

  - Agitate with ultrasound for 30 minutes in LPS (20% soln., 65o C). Lift and plunge the tray of tubes 3 times every 10 minutes.

  - RO water rinsing:

    - Plunge and lift the rack in the large rinsing tank (plastic), 10 times for a total time of 1 minute. Repeat rinse in 2nd tank.

    - Hang the rack in the large ultrasonic cleaning tank. Agitate with ultrasound for 15 minutes. Lift and plunge 5 times every 5 min.

  - Citranox bath, (10% soln., 65C) with US for 30 min. Lift and plunge the tray of tubes 3 times every 10 minutes.

  - RO water rinsing:

    - Plunge and lift the rack in the large rinsing tank (plastic), 10 times for a total time of 1 minute. Repeat rinse in 2nd tank.

    - Hang the rack in the large ultrasonic tank. Agitate with ultrasound for 15 minutes. Lift and plunge 5 times every 5 min.

- – 2nd Cycle –

  - Agitate with ultrasound for 30 minutes in warm (65o C) 20% LPS. Lift and plunge the tray of tubes 3 times every 10 minutes.

  - RO water rinsing:

Plunge and lift the rack in the large rinsing tank (plastic), 10 times for a total time of 1 minute. Repeat rinse in 2nd tank.

  - Hang the rack in the large ultrasonic cleaning tank. Agitate with ultrasound for 15 minutes. Lift and plunge 5 times every 5 minutes.

  - Prepare a fresh Citranox bath, (0.5% soln., 65C) in the insert tray. Place this tray in the deep ultrasonic tank. Process with US for 1 min. Remove the insert tray when finished.

    - RO water rinsing:

Rinse with RO in the large ultrasonic tank for 1 minute.

    - Re-fill the 2 plastic rinsing tanks with RO. Plunge and lift the rack in 10 times in each tank.

  - Final Step: Dip the rack in Ethanol Bath 1 for 30 seconds. Lift and allow to drain. Dip the rack in Ethanol Bath 2 for 30 seconds. Stand to drain. Blow down each tube with nitrogen, and then blow off exterior of tubes.

- Stand to dry.

- Perform Quality Control of Tube Cleaning procedure.

- Package passed clean tubes for storage by carefully placing the batch of tubes in a polybag, fill the bag with nitrogen gas, and then seal the bag closed. Label the bag with Date, & Batch Number. Store the bag in the cleanroom on the shelf designated for tube storage.

- Complete the Tube Processing Tag and ensure the Materials Cleaning Report is completed.