##### Process Spec:		Procedure for Tube Cleaning - Rewash

Components:		Copper Tubes

Materials:			Latex Gloves, Heavy Chemical Gloves

### Citranox Cleaner, LPS Cleaner

Reverse Osmosis Water, Foam swabs

Tooling:			Ultrasonic Cleaners

Cleaning Racks, Rinsing Tanks, Bag heat sealer

QC Data Sheet:		Quality Control of Tube Cleaning

###### Materials Cleaning Report

Tube Processing Tag

Process:

This Sheet defines the process for rewashing tubes rejected during the QC swabbing.

Wear gloves whenever tubes are being handled.  Heavy chemical gloves can be worn when handling hot objects, or when handling mineral spirits.

  - Agitate with ultrasound for 5 minutes in warm (65o C) 20% LPS.

  - RO water rinsing:

    - Plunge and lift the rack in the large rinsing tank (plastic), 10 times for a total time of 1 minute. Repeat rinse in 2nd tank.

    - Hang the rack in the large ultrasonic cleaning tank. Agitate with ultrasound for 5 minutes.

  - Prepare a fresh Citranox bath, (0.1% solution., 65C) in the insert tray. Place this tray in the deep ultrasonic tank. Process with US for 1 min. Remove the insert tray when finished.

  - RO water rinsing:

    - Rinse with RO in the large ultrasonic tank for 1 minute.

    - Re-fill the 2 plastic rinsing tanks with RO. Plunge and lift the rack in 10 times in each tank.

- Dip the rack in Ethanol Bath 1 for 30 seconds. Lift and allow to drain. Dip the rack in Ethanol Bath 2 for 30 seconds. Stand to drain. Blow down each tube with nitrogen, and then blow off exterior of tubes.

- Stand to dry.

- Perform Quality Control of Tube Cleaning procedure.

- Package passed clean tubes for storage by carefully placing the batch of tubes in a polybag, fill the bag with nitrogen gas, and then seal the bag closed. Label the bag with Date, & Batch Number. Store the bag in the cleanroom on the shelf designated for tube storage.

- Complete the Tube Processing Tag and ensure the Materials Cleaning Report is completed.