Process Spec:		Quality Control of Tube Cleaning

Components:		Copper Tubes

Material:			Latex Gloves

Ethanol

Foam Swab

Tooling:			Magnifying Lens

Swab holder

Parts Bins

QC Data Sheet:		Materials Cleaning Report

Process:

- Following the cleaning process, every tube must be swabbed.

- Wipe down the inner bore with a foam swab dipped in ethanol.

- With the lens examine the swab for traces of grease, dirt or metal flakes.

- If the swab is clean of all contamination, place the tube in the Pass bin.

- If the swab shows yellow contamination only, place the tube in the Yellow bin for re-cleaning in the Citranox & final rinse stages.

- If the tube swab shows brown, copper or grease, swab a second time.

- If the 2nd swab is clean of any contamination, place tube in the Pass bin.

- If the swab shows any contamination, place the tube in the Rewash bin.

- Dry tubes immediately after swabbing.

- Continue swabbing all tubes in the batch.

- Ensure the Materials Cleaning Report is completed.

#### QC/QA SWABBING & EVALUATION FLOWCHART

# Text boxes

PRE-SOAK

& SWAB

ULTRASONIC CLEANING PROCESS

QC /QA

1ST  SWAB

IS THE SWAB CLEAN?

QC /QA

2ND  SWAB

IS THE SWAB CLEAN?

N

Y

Y

N

### PASS