Process Spec:		Procedure for Ground Pin Insertion

Components:		Endplate

Ground Pins

Material:			Latex Gloves

Cleanroom Wipes

Ethanol

Tooling:			Ground Pin Insertion Tool

Yellow Parts Bin

QC Data Sheet:		Assembly Logbook

Process:

- This procedure is to be performed in the cleanroom.

- Select a ground pin and load it into the pin insertion tool.

- Position the pin over the ground hole.

- Carefully hold the tool perpendicular to the face of the endplate and push on the tool to insert the pin, usually 3 or 4 strokes, until the shoulder is flush with the surface. Be careful not to over-insert the pin.

- Inspect the insertion. The pin should be fully inserted and straight. Remove any damaged or improperly inserted pins.

- Record competed pin insertions in the Assembly Logbook.