Process Spec:	Procedure for Interconnect Board Assembly

Components:		Readout Printed Circuit Boards

Receptacles

Material:			Solder, "44" Rosin Core

Cotton Gloves

Tooling:			Soldering Iron

Magnifying Lamp

Soldering Jig

QC Data Sheet:

Process:

- Wear cotton gloves throughout this process.

- Refer to the printed drawing of the ICB with component notation and to the prepared sample Assembled ICB.

- Mount a ICB in the Soldering Jig, with the signal track side up.

- Insert 10 receptacles into the ICB, with the shoulder of the receptacle on the signal side of the ICB.

- Hand-solder each socket to board, ensuring that a solder meniscus is created around entire circumference of socket. Take care that no solder enters the inside of the receptacle.

- Flip the ICB over and solder other side of the ICB.

- Visually inspect soldering under magnifying lamp. Re-solder if necessary.