Process Spec:		Procedure for Washer Installation

Components:		Retaining Washers, Lozenge

Retaining Washers, Lock

Material:			Latex Gloves

Cleanroom Wipes

Ethanol

Tooling:			Lock washer installation tools

QC Data Sheet:		Assembly Logbook

Process:

- This procedure is to be performed in the cleanroom.

- Select a “lozenge” washer, place it over the pins, and push it on until it rests above the pin’s retaining shoulder.

- Select a “lock” washer, and push it on until it catches above the pin’s retaining shoulder.

- During this procedure, take care to align the fibre so that it contacts the edge of the board. Do not allow the fibre to become bent and trapped under the washer.

- Record the completed work in the Assembly Logbook.