Process Spec:		Endplate Cleaning

Components:		Matrix plates

Material:			Cotton Gloves

## Latex Gloves

Citranox

LPS Precision Clean

Tooling:			Ultrasonic Plate Cleaning Tank

Plate Transport Cart

Plate Hoisting Fixture

QC Data Sheet:

Process:

- Wear cotton gloves whenever handling plates. Switch to latex gloves when plates are clean.

- Using Plate Hoisting Fixture, move plate into Ultrasonic Plate Cleaning Tank.

- Fill tank with room temperature LPS solution (1:50) until plate is completely submerged.  Soak overnight.

- Heat tank to 60( C, then run ultrasonic agitator for two hours.

- Drain tank, reserve solution for re-use.

- Rinse plate by running water over plate using hand held hose.  Rinse for one minute.

- Fill tank with Citranox solution (1:50) until plate is completely submerged.  Heat tank to 60( C, then run ultrasonic agitator for two hours.

- Drain tank, reserve solution for re-use.

- Rinse plate by running water over plate using hand held hose.  Rinse for one minute.

- Lift plate from tank and leave plate suspended above tank on hoist.

- Dry plate with compressed air using air nozzle.  Blow out each hole until dry.

- Using hoist, place plate on transport cart for move into clean room.