Process Spec:		Cleaning Miscellaneous Hardware

Components:		Miscellaneous Hardware

Material:			Latex Gloves

Heavy Chemical Gloves

Citranox Cleaner

LPS Cleaner

Ethanol

RO Water

Clean Room Wipes

Tooling:			Ultrasonic Cleaner

Blow Dryer

QC Data Sheet:		Materials Cleaning Report

Process:

- Agitate in warm (60o C) 5% LPS solution with ultrasound for 30 minutes

- Rinse in RO (reverse osmosis water) for 5 minutes.

- Agitate in warm (60o C) 2% Citranox solution for 30 minutes.

- Rinse in RO water for 5 minutes.

- Rinse in ethanol baths for 1 minute.

- Dry with blow dryer.

- Package cleaned items in clean sealed plastic bags.

- Store packaged parts in cleanroom.

- Complete the Materials Cleaning Report.