Process Spec:		Procedure for Tungsten Rod Preparation

Components:		Tungsten Rods

Material:			Latex Gloves, Heavy Chemical Gloves

Citranox Cleaner, LPS Cleaner, RO Water

Shop Towels, Micro-Swabs, Ethanol

Tooling:			High Pressure Washer

## Ultrasonic Bath,

## Plastic Plunge Tanks

Rod Washing Racks,

Parts Bins, Shop Microscope

QC Data Sheet:		Rod Processing Tag

Process:

- Initial Cleaning

Wipe:

  - After drilling, use a shop paper towel, to wipe each rod to remove grease.

  - Use a micro swab to clear out the drill hole.

High Pressure Washer:

  - Load each drilled

  - rod into the High Pressure Washer and spray the drilled hole for 30 seconds. If both ends of the rod are drilled, then spray both ends.

  - Wipe dry the rod and blow out the hole with compressed air. When you have completed this step on the whole batch, sign-off on the 3rd step on the Rod Processing Tag.

  - 1st QC Swab: With a micro-swab and ethanol, wipe out the hole of each rod. Use the same swab until the swab locks dirty, then use a fresh swab, and so on. Examine the swab.

  - If the drill hole is obviously dirty (i.e. visible to the naked eye), repeat from Step 2.1.

  - Place washed rods in tray, sign-off on the 4th step on the Rod Processing Tag, and pass the batch on for Drill Hole Inspection.

- Ultrasonic cleaning:

  - Load a batch of 72 rods into the washing rack, hole end down.

  - Agitate in 5% LPS solution (60o C) with ultrasound for 10 minutes, with rods horizontal.

  - Rinse in RO water with 10 plunges in 1st tank followed by 10 plunges in the 2nd tank.

  - Agitate in RO water with ultrasound for 5 minutes with the rods vertical, hole end down. Followed by 5 minutes in the same tank, rods horizontal.

  - Agitate in 2% Citranox solution (60o C) with ultrasound for 10 minutes, rods horizontal.

  - Rinse in RO water with 10 plunges in 1st tank followed by 10 plunges in the 2nd tank.

  - Agitate in RO water with ultrasound for 5 minutes with the rods vertical, hole end down. Followed by 5 minutes with the rods vertical, hole end down.

  - Dip in 2 baths of ethanol, 1 minute each, and stand to dry. Blow out drill holes with compressed air or nitrogen.

  - When you have completed this step on the whole batch, sign-off on the 6th step on the Rod Processing Tag.

- 2nd QC Swabbing

  - Choose 7 rods from each batch to QC swab.

  - Dip micro-swab in ethanol and swab out the drill hole. Use a fresh swab for each hole.

  - Examine the swab under the magnifier lamp. The rod hole is judged to be dirty if there is a visible amount of dirt on the swab. Re-swab any dirty drill holes found. Examine one of the 7 swabs (choose the “most suspicious” swab) under microscope to see if there are traces of dirt on the swab. If 3 or more holes of the 7 sample rods are dirty, then swab the entire batch.

  - Place passed clean rods in a bag, add label, and seal with twist tie. Store on the designated shelf.

  - When you have completed this step on the whole batch, sign-off on the 7th step on the Rod Processing Tag.