Process Spec:	 	Procedure for Tube Deburring

Components:		Copper Tubes

Materials:			latex/nitrile gloves

Tools:			Drill press with tube jig

Chamfering Tool, Emery Paper

Dremel Tool with Felt Polisher

## Parts Bins, Nylon disk power brush

QC Data Sheet:		Tube Processing Tag

Tube Deburring Logbook

Process:

- Wear gloves and safety glasses during this procedure.

- Obtain a carton of received & inspected copper tubes.

- Chamfer both ends of the tubes using the drill press with the chamfering tool. Use very light pressure.

- Wipe both ends of the tubes with the emery paper. Use heavy pressure.

- Polish both ends of the tubes with the Dremel felt polisher. Use moderate pressure.

- Brush each end of the tube using the nylon disk brush. Use moderate pressure.

- Carefully place processed tubes into the Parts Bin.

- Ensure that the Tube Processing Tag is initiated. Place the Tag into the bin with the tubes.

- Process a batch of 124 tubes in this manner.

- Check the bit for signs of wear. Use the deburring cutter for 1000 tubes or until it shows signs of wear.

- Brush the bit and use a drop of cutting fluid after every 10 tubes.

- Pass the bin of tubes onto the Tube Deburring Inspection station.

- Fill in the Tube Processing Tag and record your work in the Tube Deburring Logbook.